TABLE 5-B

MINIMUM REQUIREMENTS FOR STRUCTURAL

COMPOSITION OF PAVEMENTS

Street	Flexible Pavements	Rigid Pavements

Classification	Alt. #1	Alt. #2		Alt. #1	Alt. #2

MARGINAL	4” BAM	8” Cr. St.	6” P.C.C.	---------

LAND ACCESS	2” I-11 Surf.	1 ½” I-11 Bind.	(15’ Plain Jts)

Residential		1 ½” I-11 Surf.

LOCAL	5” BAM	8” Cr. St.	6” P.C.C.	---------

Residential	2” I-11 Surf.	2” I-11 Bind.	(15’ Plain Jts)

1 ½” I-11 Surf.

COLLECTOR	4” BAM	8” Cr. St.	6” S.R.P.C.C.	5” P.C.C.

Residential	2 ½” I-11 Bind.	3” BAM	(40’ Dowell Jts)	4” Cr. St./

2” I-11 Surf.	1 ½” I-11 Surf.			U.L. (15’

Dowel Jts)

LOCAL	4” BAM	8” Cr. St.	6” S.R.P.C.C.	6” P.C.C.

Commercial and	2” I-11 Bind.	3” BAM	(40’ Dowel Jts)	4” Cr. St./

Industrial	1 ½” I-11 Surf.	2” I-11 Surf.			U.L. (15’

Dowel Jts)

COLLECTOR	6” BAM	8” Cr. St.	7” S.R.P.C.C.	-------------

Commercial and	2 ½” I-11 Bind.	4” BAM	(40’ Dowel Jts)

Industrial	1 ½” I-11 Surf.	1 ½” I-11 Bind.	4” Cr. St./U.L.

1 ½” I-11 Surf.

NOTE:	Equivalent pavements in addition to those shown above shall be determined by the City Engineer.  Should the total pavement thickness exceed 8” the granular base/subbase shall extend under the curb/gutter.

ABBREVIATIONS:

Cr. St.		=	Crushed Stone

BAM		=	Bituminous Aggregate Mixture

U.L.		=	Underlayment

P.C.C.		=	Unreinforced Portland Cement Concrete

S.R.P.C.C.	=	Standard Reinforced Portland Cement Concrete

MAXIMUM LIFT THICKNESS:

Crushed Stone	=	8”

BAM		=	6”

I-11 Binder	=	2 ½”

I-11 Surface	=	2”